## Slide 1: can we recover 0.2eV of open circuit voltage?
Nir Tessler, Lior Tzabari
Microelectronic and Nanoelectronic Centers,
Electrical Engineering Department,
Technion Israel Institute of Technology,
Haifa 32000, Israel

## Slide 2
Outline
What we (slowly) learned over the years about BHJ
(Power dependent QE method)
Maybe the fault is in the device structure and not the materials
(Contact Engineering)

## Slide 3
Some of the processes in
P3HT-ICBA Devices
+
-
- +
+
-
+
-
Anode (positive contact)
+
+
-
-
Light
Exciton
Charge transfer
Exciton
Free charges
Generation
Loss
Light emission
Charge recombination
Polaron-Exciton
annihilation

## Slide 4
+ -
- +
-
+
-
+
+ -
+
- +
+
The Physical Framework we built
L. Tzabari, V. Zayats and N. Tessler; J. Appl. Phys. 114, 154514 (2013)

## Slide 5: Shockley-Read-Hall (SRH) recombination
Capture cross section is as in Langevin recombination
Kuik, M., et. al. Physical Review Letters, 107(25), 256805, (2011).

## Slide 6
HOMO
LUMO
Donor
HOMO
LUMO
Acceptor
+ Charge transfer state -
Free polaron
Eb
Polaron pair (CT)
ECT
Ground state
LUMO
HOMO
Eg/2
Traps
EFi
DEt
Eb
Valence band
Conduction band
3 Simplifications
1. Effective electronic band gap
2. CT states = charge recombination traps
3. CT (trap) of narrow energy band (1 level)
L. Tzabari, et. al., "The Role of Charge Transfer States …. ," J Phys Chem C, 2014.
R. A. Street, Advanced Functional Materials, 22(21), 4608–4619 2012

## Slide 7: Model’s Equations
Notation:

## Slide 8
Time resolved pump-probe techniques
Typically all excitations are found to decay within a ms.
External quantum efficiency of solar cells
Sometimes excitations live up to milliseconds
Log t
Log P

## Slide 9
Equilibrium? Steady state?
Chain morphology?
Cubic lattice
Chain morphology
Chain + 4 site conjugation
Mobility
When we apply Electric field
Charges go up in energy
Effective temperature of e-
mobility
Polymers have higher tendency towards “quasi” equilibrium
D. Mendels & N. Tessler, Scientific reports , to be published.
Why CW ?

## Slide 10
Efficient charge generation by relaxed charge-transfer states at organic interfaces.
Koen Vandewal,…., Alberto Salleo; Nature Mat, 2014, 13, 63-68.
There are lots of processes on the sub ns time scale. But by the time the device cares about it - all populations are at quasi equilibrium
Why CW ?

## Slide 11
Cell Efficiency
Generating Power (mWcm-2)
HOMO
Glass
ITO
PEDOT:PSS
Ca
Al
Free-Charge
Generation Efficiency
Other Losses Kick in
N. Tessler and N. Rappaport, JAP, vol. 96, pp. 1083-1087, 2004.
N. Rappaport, et. al., JAP, vol. 98, p. 033714, 2005.
QE as a function of excitation power @ VSC

## Slide 12
N. Tessler and N. Rappaport, Journal of Applied Physics, vol. 96, pp. 1083-1087, 2004.
N. Rappaport, et. al., Journal of Applied Physics, vol. 98, p. 033714, 2005.
Signature of
bi-molecular Loss
Smaller Bimolecular Coefficient
Signature of bi-molecular loss mechanism

## Slide 13
Fewer Traps
Deeper Traps
L. Tzabari, and N. Tessler, J Appl Phys 109, 064501 (2011)
L. Tzabari, et. al., J Appl Phys, vol. 114, p. 154514, 2013.
SRH Recombination
- QE as a Function of Light Intensity
LUMO
HOMO
dEt
Notes: The SRH recombination in the context of blends describes the fact that in a BHJ an electron-hole recombination can occur only at specific spatial location (the interface between the two phases) and through certain energy levels (CT states). Those sites will be treated as the SRH recombination centers (the "traps"). Their density will reflect the interface density, and their depth will follow the system energetic levels. This process starts as a bimolecular process (hence the drop) and as the recombination centers are filled it becomes monomolecular and its effect on the QE saturates. Therefore the clear signature of SRH is mainly visible at the low excitation regime.

## Slide 14: Fitting procedure
Vapp
SRH
Bimolecular
Normalization is done to the absolute value at the low intensity regime of the Vapp=0V curve.

## Slide 15: Fitting procedure
(c)
(d)
(e)
(f)
(a)
(b)
6.5e15cm-3
9.5e15cm-3
CT density
9.5e14cm-3
3.5e14cm-3
7.5e14cm-3
Dark carrier density
3e3
3e4

## Slide 16: Fast Dry vs. Slow Dry (CB vs. DCB)
L. Tzabari, et. al., J. Phys. Chem. C, 120(19), 10146–10155, 2016..
.
What else is there?
Traps are FULL
Electrochemical potential difference should be high
Notes: Examining the results we suggest that the SRH recombination centers are the Charge Transfer States (CT's) at the interface between the different phases. The CT's are used at the same time as a generation center for exciton dissociation, and as a recombination pathway for free carriers. As the CT's density is a function of the phase segregation in the active layer, we claim that our findings indicate that using the slow dry process results in finer phase segregation.
It is important to note that although exhibiting more SRH loss, the slow dry devices are more efficient than the fast dry ones due to their higher generation efficiency which results from the same CT's that cause the recombination loss. The relative overall generation efficiency can be extracted from the plateau in the not normalized QE graph

## Slide 17: Electrochemical Pot. Diff.?
0.2 eV ?
Donor HOMO
Acceptor LUMO
CT binding energy = Trap
Molecular Picture
VOC=0.8 V
Dm ≥ 1.0 eV

## Slide 18: Semiconductor Device Model What happens @ VOC?
0.16V at the Contact + 0.04V in the Bulk = 0.2 V
V=VOC
L. Tzabari, et. al., J Phys Chem C, 118(48), 27681–27689 (2014).
V. D Mihailetchi et. al. Journal of Applied Physics, 94(10), 6849–6854. (2003).
T. Kirchartz, et. al., Journal of Physical Chemistry Letters, 4(14), 2371–2376. (2013).
It is not just a possibility the device is actually doing it!

## Slide 19
The effect of pinned electrodes
Liu, B., (2014). Advanced Energy Materials, 4(4), 1200972.
Vbi limits VOC

## Slide 20
0.81+0.037*ln(S)
0.60+0.040*ln(S)
Open Circuit
P3HT-ICBA
P3HT-PCBM
Move to full device model
Tessler, N. “Adding 0.2 V to….” Journal of Applied Physics, 118(21), 215501. (2015).
Tessler, N. “Experimental techniques and…” J. Poly. Sc. B, 52(17), 1119–1152. (2014).
(making sure it reproduces real device data)
Short Circuit

## Slide 21
LUMO
HOMO
LUMO
HOMO
LUMO
HOMO
LUMO
HOMO
Higher Built-in Potential
Can we add %% to PCE
PCBM
Bis-PCBM
ICBA

## Slide 22
We often observe that improving materials affects only FF
Reducing bulk losses x 10

## Slide 23
CnNt=3.3x104s-1
Standard, 0eV
0.2eV
0.3eV
LUMO, Conduction
HOMO, Valence
P3HT:ICBA
25% increase in PCE
+ 0.1V

## Slide 24
CnNt=3.3x103s-1
Standard, 0eV
0.2eV
0.3eV
Something slightly better than P3HT
48% increase in PCE
+ 0.2V in VOC

## Slide 25
Standard
Structure
Band gap enhanced
structure
Comparing Materials ?
Can’t always just blame the chemist

## Slide 26
-
+
Full Device Model
EFh
EFe
EG =1.36
Vbi=1.56
VOC=1V

## Slide 27: Thank You
The fabrication was performed at the Micro-Nano Fabrication Unit (MNFU), Technion.
Israel Science Foundation
INNI Focal Technical Area on Nano-Photonics
Intensity dependent QE is a powerful tool & simple model
Contact Engineering can recover FF, ISC, & 0.2V of VOC
Summary
Collaborations
  Prof Julia WP Hsu (University of Texas at Dallas)
  Jian Wang
  Yun-Ju Lee