## Slide 1: Dan Mendels, Nir Tessler
Sara & Moshe Zisapel Nanoelectronic Center
Electrical Engineering Dept.
Haifa 32000
Israel
www.ee.technion.ac.il/nir
Mobility and Diffusion under the Premise of Solar Cells
The Role of Energy-Transport

## Slide 2
The operation of Solar Cells is all about balancing nergy
Think “high density” or “many charges” NOT “single charge”
There is extra energy embedded in the ensemble
If you came from session P.
There is also pseudo band like behavior

## Slide 3: The Physical Framework
Steady State I-V measurements
Steady State  Qausi Equilibrium (Incl. Traps)
Not the transient, possibly dispersive, transport where D/m may be VERY HIGH
R. Richert, L. Pautmeier, and H. Bassler, "Diffusion and drift of charge-carriers in a random potential - deviation from Einstein law," Phys. Rev. Lett., vol. 63, pp. 547-550, 1989.
[1] K. C. Kao and W. Hwang, Electrical transport in solids vol. 14. New York: Pergamon press, 1981.
[2] H. T. Nicolai, M. M. Mandoc, and P. W. M. Blom, "Electron traps in semiconducting polymers…" PRB, 83, 195204, 2011.

## Slide 4: Original Motivation
Measure Diodes I-V
Extract the ideality factor
The ideality factor
Is the Generalized Einstein Relation
The Generalized Einstein Relation is NOT valid for
organic semiconductors
Y. Vaynzof et. al. JAP, vol. 106, p. 6, Oct 2009.
G. A. H. Wetzelaer, et. al., "Validity of the Einstein Relation in Disordered Organic Semiconductors," PRL, 107, p. 066605, 2011.

## Slide 5
Monte-Carlo simulation of transport
G.E.R.
Monte-Carlo
Standard M.C. means uniform density
Y. Roichman and N. Tessler, "Generalized Einstein relation for disordered semiconductors - Implications for device performance," APL, 80, 1948, 2002.

## Slide 6: Comparing Monte-Carlo to Drift-Diffusion & Generalized Einstein Relation
qE
qE
Implement contacts as in real Devices
GER Holds for real device Monte-Carlo Simulation

## Slide 7: Where does most of the confusion come from
J. Bisquert, Physical Chemistry Chemical Physics, vol. 10, pp. 3175-3194, 2008.
D The intuitive Random Walk
The coefficient describing
Generalized Einstein Relation is defined ONLY for

## Slide 8: What is Hiding behind
E
X
E
X
Charges move from high density region to low density region
Charges with High Energy move from high density region to low density
There is an Energy Transport

## Slide 9: The Energy Balance Equation
The operation of Solar Cells is all about balancing nergy
DE
R

## Slide 10
s=3kT
DOS = 1021cm-3
N=5x1017cm-3=5x10-4 DOS
Low Electric Field
B. Hartenstein and H. Bassler, Journal of Non - Crystalline Solids 190, 112 (1995).
How much “Excess” energy is there?
150meV

## Slide 11: The High Density Picture Mobile and Immobile Carriers
Mobile Carriers
s=3kT
DOS = 1021cm-3
N=5x1017cm-3=5x10-4 DOS
Low Electric Field
Transport is carried by high energy carriers
Is it a BAND?
Jumps distribution

## Slide 12: Summary
Transport: Many Charges ≠ Single Charge
  Mobile and Immobile (“trapped”, “Band”) charges
Transport of energy!
  There is “excess” energy in the system.
Where do the carriers hop in energy
  Not around EF.
Ideality factor Einstein relation?
Seebeck
Effect
Recombination
Thank You

## Slide 13
e
Mott’s Variable Range Hopping
Effective initial energy
Effective intermediate energy
DE
For a constant density of states:
For a shaped density of states:
Transport Energy (Et=?)
r and DE are determined so as to maximize the hopping rate
E
r

## Slide 14
Transport Energy
Effective Initial Energy
KBT
1. Mobility is charge density dependent
2.
3. is
There is transport of energy even in the absence of Temperature gradients
(a)

## Slide 15: What if we analyze the standard (uniform density) Monte-Carlo
GER
Monte-Carlo

## Slide 16
e- & E

## Slide 17
Does the Generalized Einstein Apply
Does your system obey the laws
of Thermodynamics