## Slide 1
We claim – in our system all states are localized. Why?
x
e

## Slide 2: Few General Concepts
The physical scene we would be interested in

## Slide 3
Z
Creating electronic continuity
E
E1
P
0
Wave-functions of first confined states
( probability to find electron at z = z0)
( Energy level of the state )
Spatial proximity leads to wave-function overlap.
E11
E12
E1
E1
E11
E12
(a)
(b)
(c)
The distance determines the strength of the overlap or DE=E12-E11.

## Slide 4
E1
E1*
E11
E12
E1
E1*
E11
E12
E1
E1*
E11
E12
E1
E1*
E11
E12
Two states are equally shared by the sites
Two states are separate
(Two identical pendulum in resonance)
(Very different pendulum do not resonate - stronger disorder)
Strong coupling overcomes minute differences (low disorder)

## Slide 5
E0
E0
E0
+
r1
E0
E0
+
r2
E0
E0
E0
+
r1
E0
E0
+
r2
+
r3
+
E1
E2
E3
E4
No long range “resonance”
Lifshitz Localization
If there is a large disorder in the spatial coordinates  no band is formed and the states are localized.

## Slide 6
Conjugation length
Long
Short
Varying chain distance
Strong coupling
Weak coupling
Coupling also affected by relative alignment of the chains (dipole)
parallel
shift
tilt

## Slide 7: Localization in “Soft” matter

## Slide 8
Polymers: carbon based long repeating molecules
-conjugation: double bond conjugation
What are conjugated polymers?
MEH-PPV
poly[acetylene]
Molecular organic
Semiconductor
C
C
H
H
C
C
H
H
C
C
H
H
C
C
H
H
C
C
H
H

## Slide 9: Conjugation

## Slide 11
+
+
-
-
p-
p+
p-
p+
Bonding

=
p-
p+
p+
p-
+
+
-
-
Anti-bonding
*
=
Z
Amplitude
p+
p-
The phase of the
wave function
Molecular p levels
Stable state
Less Stable state
Consider 2 atoms

## Slide 12
4 atoms
HOMO
(Valence)
LUMO
(Conduction)
There is correlation between spatial coordinates and the electronic configuration!!

## Slide 13
Molecule’s
Length
Energy
Configuration coordinate

## Slide 14
c
c
c
c
c
c
c
c
c
c
Sigma
p
Dimerised (1)
Dimerised (2)
(a)
(b)
(c)
(d)
(
b)
(
c)
(
d)
Energy
(
b)
(
c)
(
d)
Energy
Bond Length
Degenerate ground state
Another coordinate system

## Slide 15
Aromatic link
Quinoidal link
General or schematic configuration coordinate

## Slide 16
The potential at the bottom of the well is ~parabolic (spring like)

## Slide 17
Q0
E0spring
E=E0+B(Q-Q0)2
Spring Energy

## Slide 18
Elastic energy:
Equilibrium
Stretched
Squeezed
Simplistic approach

## Slide 19
Q0
E0t= E0spring+E0elec
Q
Here, the particle just entered the system (molecule) and we see the state before the environment responded to its presence (prior to relaxation)
The system relaxed to a new equilibrium state. In the process there was an increase in elastic energy of the environment and the electron’s energy went down. On the overall energy was released (typically) as heat.
Adding a particle will raise the system’s energy by (m*g*h)
On a 2D surface
The particle dug himself a hole
(self localization)

## Slide 20
Q0
E0spring
Q
A
A*
A
A*
If the potential energy of the mass would not depend on its vertical position

## Slide 21
Q
A*
A*
If the potential energy of the mass would not depend on its vertical position
A’
We’ll be interested in the phenomena arising from the relation between the length of the spring and the particle’s potential energy.
We’ll claim that due to this phenomenon there the system (electron) will be stabilized

## Slide 22
L
L + dL
Stretch mode
En
En +dEn
For small variations in the “size” of the molecule the electron phonon contribution to the energy of the electron is linear with the displacement of the molecular coordinates.
For p-conjugated the atomic displacement is ~0.1A and F=2-3eV/A.
The general formalism:
Ee-ph=-AQ

## Slide 23
Linear electron-phonon interaction:
The system was stabilized by DE through electron-phonon interaction 
Polaron binding energy

## Slide 24
Molecule without e-ph relaxation
Molecule with e-ph relaxation
What is the energy change, at Qmin, due to reorganization?
“stretch” the molecule to the configuration associated with the e-ph relaxation and see how much is gained by the e-ph relaxation.
What is l ?

## Slide 25
Why all this is relevant to charge transport?

## Slide 26
Molecule without a charge
Molecule containing a charge
If the two molecules are identical and have the same E0 
The electron carries En+AQ1 and replace it with En+AQ2 
Transfer is most likely to occur when Q1=Q2=Q
Total excess energy to reach this state:
Transfer will occur when by moving the electron from one molecule to other there would be no change in total energy.

## Slide 27
Transfer will occur when Q1=Q2=Q
Total excess energy to reach this state:
Electron transfer is thermally activated process
Typical number is:
To move an electron or activate the transport we need energy of:

## Slide 28
E
Q
E
EC
Polaron Binding Energy

## Slide 29
So far we looked into:
A  A*
Let’s look at the entire transport reaction:
A + D*  A* + D

## Slide 30
E
Q1
E
Q2
E
Q*
Two separate molecules
One reaction or system

## Slide 31
A system that is made of two identical molecules
As the molecules are identical it will be symmetric (the state where charge is on molecule A is equivalent to the state where charge is on molecule D)

## Slide 32
l
l
Wa
l=4Wa=2Eb
If the reactants and the products have the same parabolic approximation:

## Slide 33
-1000
0
1000
2000
3000
4000
5000
6000
E
Q*
A system that is made of two identical molecules
As the molecules are identical it will be symmetric (charge on A is equivalent to charge on D)
Wa
D
A
D
A
Reactants
Products

## Slide 34
Average
attempt frequency
Activation of the molecular conformation
Probability of electron to move (tunnel) between two “similar” molecules
Requires the “presence” of phonons.
Or the occupation of the relevant phonons should be significant

## Slide 35
What is a Phonon?
Considering the regular lattice of atoms in a uniform solid material, you would expect there to be energy associated with the vibrations of these atoms. But they are tied together with bonds, so they can't vibrate independently. The vibrations take the form of collective modes which propagate through the material. Such propagating lattice vibrations can be considered to be sound waves, and their propagation speed is the speed of sound in the material.
The vibrational energies of molecules, e.g., a diatomic molecule, are quantized and treated as quantum harmonic oscillators. Quantum harmonic oscillators have equally spaced energy levels with separation DE = hu. So the oscillators can accept or lose energy only in discrete units of energy hu.
The evidence on the behavior of vibrational energy in periodic solids is that the collective vibrational modes can accept energy only in discrete amounts, and these quanta of energy have been labeled "phonons". Like the photons of electromagnetic energy, they obey Bose-Einstein statistics.

## Slide 36
Considering a “regular” solid which is a periodic array of mass points, there are “simple” constraints imposed by the structure on the vibrational modes.
Such finite size (L) lattice creates a square-well potential with discrete modes.
Associating a phonon energy
vs is the speed of sound in the solid

## Slide 37
Configuration
Co-ordinate
Energy
0
1
2
0
1
2
Configuration
Co-ordinate
Energy
Q
Q
For a complex molecule with many degrees of freedom we use the configuration co-ordinate notation:
For the molecule to reach larger Q – higher energy phonons states should be populated

## Slide 38: Bosons:
What will happen if T<Tphonon/2
In the context of:
The relevance to our average attempt frequency:

## Slide 39
-1000
0
1000
2000
3000
4000
5000
6000
E
Q
A system that is made of two identical molecules
At low temperature the probability to acquire enough energy to bring the two molecules to the top of the barrier is VERY low.
In this case the electron may be exchanged at “non-ideal” configuration of the atoms or in other words there would be tunneling in the atoms configuration (atoms tunnel!).
[D. Emin, "Phonon-Assisted Jump Rate in Noncrystalline Solids," Physical Review Letters, vol. 32, pp. 303-307, 1974].
Wa
A
B
A
B
Would the electron transfer rate still follow exp(-qWa/kT)

## Slide 40
High T regime:
~200k in polymers
Activation energy decreases with Temperature
[N. Tessler, Y. Preezant, N. Rappaport, and Y. Roichman, "Charge Transport in Disordered Organic Materials and Its Relevance to Thin-Film Devices: A Tutorial Review," Advanced Materials, vol. 21, pp. 2741-2761, Jul 2009.]

## Slide 41
Are we interested in identical molecules?
(same A, B & E0)
x
e
Consider variations in E0

## Slide 42
l
DG1
DG0
qR
qP
qc
l
Effect of disorder or applied electric field on the two molecule system:

## Slide 43
For polaron transfer (l=2|Eb|) :
Energy activation for going to the lower site:
In the present case for going down in energy
In the present case for going down in energy

## Slide 44
Energy activation for going to the lower site:
This term is usually negligible

## Slide 45
l
DG1
DG0=Ei-Ej
qi
qj
qc
l
Effect of disorder or applied electric field on the two molecule system:

## Slide 46
Gaussian Distribution of States
E
1017cm-3
1018cm-3
Let’s consider a system characterized by:
x
e

## Slide 47: Detailed Equilibrium
Another form:
P
V. Ambegaokar, B. I. Halperin, and J. S. Langer, "Hopping Conductivity in Disordered Systems," Phys. Rev. B, vol. 4, pp. 2612-&, 1971.
A. Miller and E. Abrahams, "Impurity Conduction at Low Concentrations," Phys. Rev., vol. 120, pp. 745-755, 1960.

## Slide 48
Under which circumstances can we use:
m and D are statistical quantities
  A. Statistics has to be well defined
  B. Variation in the structure/properties are slow compared to the length scale we are interested in
Gaussian Distribution of States
E
1017cm-3
1018cm-3
Density and spatial regime
Carrier sampling DOS