## Slide 1: Dan Mendels, Ariel Ben Sasson, Michael Greenman, Nir Yaacobi-Gross, Ariel Epstein, Nir Tessler
Sara & Moshe Zisapel Nanoelectronic Center
Electrical Engineering Dept.
Haifa 32000
Israel
www.ee.technion.ac.il/nir
Electrical Engineering Perspective of a Material Driven Field

## Slide 2: Outline
Transport (do we know it all?)
Material manipulations by EE
Engineering tool for OLED analysis
Engineering FET structure (VOFET)

## Slide 3
Technion Campus

## Slide 4: Lab to FAB
Large size companies got seriously involved at around 1997
Today, 15 years later, there are still some basics we don’t know
In the context of amorphous organic semiconductors

## Slide 5: Trivia
Chemical potential
Fermi level
Equilibrium
Drift Diffusion
Warning: each topic is dealt by at least two different communities (disciplines) that have developed their own “obvious” meaning of the terminology.

## Slide 6: Chemical Potential
Conduction
Valence
Vacuum Level
Ec
Ev
Eg
E
Chemical potential is the energy to be added to the system if an electron is added. Electron can reside either in Valence or Conduction band according to Fermi Dirac statistics. Under equilibrium it equals the parameter in the FD statistics (EF).
Equilibrium
We consider the following reaction:

## Slide 7: Quasi Chemical Potential
Conduction
Valence
Vacuum Level
Ec
Ev
E
Non-Equilibrium
Generally:
Quasi Chemical potential
≠
EF in the FD statistics (quasi - EF).
(for ideal gas they are equal)
EFh
Vacuum Level
Ec
Ev
E
EFe
QCPe
QCPh
Quasi Chemical potential is the energy to be added to the system if an electron is added. Electron can reside only in the band the quasi chemical potential refers to. In the respective band it will reside according to Fermi Dirac statistics with the respective quasi - EF.

## Slide 8: Disorder and Anderson Localization
E
x
E
Density of states
Band
Tail states (traps)
E
Density of states
Density of localized states
High Order
E
x
Low disorder
E
x
High disorder
E
Band
Density of states

## Slide 9
Transport
InGaAs
InP
DE
PFOBT
PFO
DE
R
R
When considering many
molecules or sites one uses a variant of
Mott’s Variable Range Hopping

## Slide 10
e
Mott’s Variable Range Hopping
Effective initial energy
Effective intermediate energy
DE
For a constant density of states:
For a shaped density of states:
Transport Energy (Et=?)
r and DE are determined so as to maximize the hopping rate
E
r

## Slide 11
Transport Energy
Effective Initial Energy (QCP)
KBT
J. O. Oelerich et. al. APL, 97, 143302, 2010.
D. Mendels & N. Tessler, Submitted.

## Slide 12
Transport Energy
Effective Initial Energy
KBT
1. Mobility is charge density dependent
2.
3. is
There is transport of energy even in the absence of Temperature gradients
(a)

## Slide 13
The effect is linked to charge density gradients.
Let’s examine a case where current flows and there is
no charge gradient
D/m = Einstein relation
G.E.R.
If
Seebeck effect
Monte-Carlo
new formalism
BUT
For most practical scenarios the GER is a very good approximation

## Slide 14: Engineers’ Engineering of Materials
Creating building blocks to allow for device engineering

## Slide 15
Building Electronic Materials with LEGO bricks

## Slide 16
O
O
R1
R2
Electronic Peptide
Of the shelf peptide synthesizer
Electronic Peptides
The basic idea
The materials of organic displays
The materials of Nature
Electronic-grade
Tailor-made
Yoav Eichen, Chemistry, Technion

## Slide 17
Works like a charm but for:
Amide bond is only slightly conjugated
Film morphology is difficult to control
(probably H bonds)
N. Tessler et. al., "Conjugated Polymer Electronics – Engineering Materials and Devices," in Handbook of Conducting Polymers, CRC, 2006

## Slide 18
  Colloidal nanocrystals (NCs)
Organic capping layer (Ligands)
8-18 aliphatic carbon chain
Allows solubility
Stabilizes the QDs
Act as a barrier for charge transfer
core
Greenham, N. et al. Phys Rev B, 1996, 54, 17628
Notes: Up until recently the capping layer was underestimated and was mostly looked at as to:
Allow solubility
Stabilizes the QDs
Act as a barrier for charge transfer

## Slide 19
InAs
Ligands Exchange
Y
NH2
SH
X
OCH3
CH3
NO2
Free dipole
Y
X
Y
X
Y
X
Y
X
Y
X
Y
X
Y
X
TOP
(trioctylphosphine)
Michal Soreni-Harari, et. al., Nano Lett. 8, 678-684, (2008).
Notes: Ligands exchange in order to examine the effect of the ligands dipole
We expose the NCs to high excess of competing ligands
were incubated for at least 72 h and then precipitated with methanol. After separation by centrifugation, excess ligand was removed by redispersion in toluene and precipitation with methanol

## Slide 20: HOMO level shifting (Differential Pulsed Voltammetry)
InAs
4.4 nm
TOP (original)
NH2
H
aniline
SH
CH3
MTP
-4.7eV
-4.95eV
-5.05eV
Vacuum level
Surface ligands

## Slide 21: Size Matters
4.4nm diameter
Sub 2nm diameter
Why ?

## Slide 22
CdSe
Partial Ligands Exchange
CH2(CH2)14CH3
NH2
SH
CH3
Are we polarizing
N. Yaacobi-Gross et. al. , "Molecular control of quantum-dot internal electric field …." Nat Mater, vol. 10, pp. 974-979, 2011.
Notes: Ligands exchange in order to examine the effect of the ligands dipole
were incubated for at least 72 h and then precipitated with methanol. After separation by centrifugation, excess ligand was removed by redispersion in toluene and precipitation with methanol

## Slide 23
Adding small fractions of free MTP ligands.
CH3
SH
NH2
HDA
CdSe
Mixed Ligands CdSe
Nir Yaacobi-Gross et. al., Nature Materials 10, 974-979 doi:10.1038/nmat3133
Mixed Ligands
 Stark Shift

## Slide 24
Ligands induced bulk heterojunction in near IR active all nanocrystals solar cells
Results:
Stark shift helps to dissociate charges

## Slide 25
Formulations
Triarylamine
PVK-Cin
Wide gap x-linkable conjugated matrix
O. Solomeshch et. al, "Electronic formulations…” Adv. Func. Mat, 16, 2095, 2006.
m=3% n=48.5% o=48.5%
Emitter (green PPV)
Transport (P3HT)
Dopant (C60Fxx)

## Slide 26
Formulations
Single pixel
two-Color OLED
(no loss of efficiency during processing)
Stable Hole injection layer
(PVK-Cin + P3HT + C60F36)
or
(PVK-Cin+ PolyTPD+C60F48)
110c in Vacuum
Patterning
X-Linking  Stability
O. Solomeshch et. al., "Electronic formulations - Photopatterning of luminescent conjugated polymers," Advanced Functional Materials, vol. 16, pp. 2095-2102, Oct 2006.
O. Solomeshch, et. al., “…Electrical Doping of Fluorinated C-60 in Conjugated Polymers," Advanced Materials, vol. 21, pp. 4456-+, Nov 2009.

## Slide 27
Engineering Tool
Simple method to extract recombination zone parameters in OLEDs

## Slide 28
Closed-form solution
Spatial broadening factor
Spectral broadening
Weak-microcavity
Image-Source
A. Epstein, N. Tessler, and P. D. Einziger,
IEEE J. Quantum Elect., 46, 9, pp. 1388-1395 (2010).
Direct-Ray
Cathode
ITO

## Slide 29
Emission zone (EZ) location effect
Very narrow emission zone
Different positions 
Emission pattern extrema
Origin: Image-Source interference (reflecting cathode)
Cathode
ITO

## Slide 30
Emission zone (EZ) width effect
Symmetrical distribution
Different widths 
“Fringe visibility” (ratio)
Origin: Image-Source interference averaged
Cathode
ITO
A. Epstein, N. Tessler, and P. D. Einziger, Opt. Lett., 35, 20, pp. 3366-3368 (2010).

## Slide 31
Blue P-OLED (CDT OLED)
Device under test
M. Roberts, K. Asada, M. Cass, C. Coward, S. King, A. Lee, M. Pintani, M. Ramon, and C. Foden, Proc. SPIE Photonics 7722, 77220C, Brussels (2010)
ITO 45nm
HIL 35nm
IL 15nm
LEP 130nm
Aluminium
‘p’ pol (TM)
‘s’ pol (TE)
Glass hemisphere (centre is at emissive area)
Glass Substrate 0.7mm
Chart: TE, 0.3mA
| 360 | 370 | 380 | 390 | 400 | 410 | 420 | 430 | 440 | 450 | 460 | 470 | 480 | 490 | 500 | 510 | 520 | 530 | 540 | 550 | 560 | 570 | 580 | 590 | 600 | 610 | 620 | 630 | 640 | 650 | 660 | 670 | 680 | 690 | 700 | 710 | 720 | 730 | 740 | 750 | 760 | 770 | 780 | 790 | 800 | 810 | 820 | 830
0s | 0.033304 | 0.0036041 | -0.046301 | -0.024594 | -0.00056825 | 0.0745 | 0.53606 | 3.8682 | 8.2756 | 10.7053 | 8.5152 | 6.9789 | 6.5028 | 6.3865 | 6.1341 | 6.0325 | 5.986 | 5.6501 | 5.0348 | 4.4317 | 3.8718 | 3.1014 | 2.5726 | 2.1006 | 1.6974 | 1.3917 | 1.0734 | 0.86696 | 0.71765 | 0.59499 | 0.47273 | 0.43144 | 0.2722 | 0.27681 | 0.26966 | 0.25052 | 0.25289 | 0.24252 | 0.36519 | 0.25063 | 0.08836 | 0.41114 | -0.03576 | -0.20079 | -0.52235 | -0.10107 | -0.1743 | -0.54039
10s | 0.0036169 | -0.040905 | -0.01675 | 0.011983 | -0.01459 | 0.1057 | 0.5688 | 3.619 | 7.5453 | 9.8966 | 8.0449 | 6.8201 | 6.7267 | 6.7617 | 6.6793 | 6.6468 | 6.6351 | 6.244 | 5.5466 | 4.8473 | 4.1333 | 3.3969 | 2.7478 | 2.2357 | 1.782 | 1.4285 | 1.1541 | 0.92292 | 0.78682 | 0.5953 | 0.52885 | 0.43779 | 0.37637 | 0.32265 | 0.30639 | 0.22363 | 0.23273 | 0.034604 | 0.4844 | 0.26701 | 0.1822 | 0.26716 | -0.074477 | -0.079111 | -0.66219 | 0.092242 | 0.28144 | -0.33619
20s | 0.024153 | 0.019024 | -0.051838 | -0.038382 | 0.017803 | 0.092207 | 0.53619 | 2.8907 | 5.6609 | 7.7472 | 7.0048 | 6.9171 | 7.7297 | 8.5554 | 8.797 | 8.9855 | 8.9672 | 8.303 | 7.2862 | 6.156 | 5.0927 | 4.0998 | 3.241 | 2.5216 | 1.9658 | 1.5811 | 1.2324 | 1.0272 | 0.86005 | 0.68325 | 0.56124 | 0.43632 | 0.30585 | 0.36572 | 0.35574 | 0.29253 | 0.33347 | 0.15607 | 0.18903 | 0.072365 | 0.28378 | 0.37377 | -0.113 | -0.10069 | -0.22122 | 0.55595 | -0.22917 | 0.39797
30s | 0.024032 | 0.0044818 | -0.015101 | -0.026097 | 0.041518 | 0.097499 | 0.41203 | 1.8401 | 3.6327 | 6.0275 | 7.1929 | 9.0321 | 11.8605 | 13.9188 | 14.6483 | 14.7938 | 14.2195 | 12.6187 | 10.5699 | 8.4827 | 6.6608 | 5.0599 | 3.8685 | 2.9253 | 2.1879 | 1.7357 | 1.3432 | 1.0526 | 0.84962 | 0.68503 | 0.54412 | 0.52031 | 0.40025 | 0.24883 | 0.30677 | 0.34736 | 0.37385 | 0.19778 | 0.61792 | 0.19455 | 0.27891 | 0.16961 | 0.15435 | 0.17794 | -0.0057954 | 0.33077 | 0.015106 | 0.63092
40s | 0.025854 | 0.031095 | -0.0070447 | 0.025093 | 0.051849 | 0.10107 | 0.29078 | 1.1548 | 2.5801 | 6.7488 | 11.6146 | 17.2233 | 23.7093 | 27.125 | 26.877 | 25.0761 | 21.9419 | 17.8368 | 13.7239 | 10.3596 | 7.5675 | 5.4853 | 4.0686 | 3.0667 | 2.2497 | 1.7984 | 1.3563 | 1.1299 | 0.94194 | 0.63324 | 0.56447 | 0.49186 | 0.45014 | 0.29731 | 0.28239 | 0.31041 | 0.45268 | 0.19413 | 0.48483 | 0.25979 | 0.44842 | 0.12012 | 0.062307 | -0.0011742 | -0.34009 | 0.10845 | -0.45015 | -0.16971
50s | 0.057336 | 0.058451 | 0.06633 | 0.046676 | 0.14392 | 0.15628 | 0.29926 | 0.80828 | 2.9886 | 13.5261 | 27.3267 | 39.8325 | 47.7587 | 45.782 | 38.4687 | 30.8101 | 24.1017 | 18.1457 | 13.1943 | 9.5757 | 6.8953 | 4.9984 | 3.7243 | 2.774 | 2.136 | 1.6443 | 1.2262 | 1.0064 | 0.87719 | 0.63401 | 0.57398 | 0.4824 | 0.40289 | 0.32202 | 0.36812 | 0.33953 | 0.4432 | 0.21809 | 0.49979 | 0.38509 | 0.46214 | 0.46385 | 0.11293 | -0.055937 | -0.1014 | 0.70167 | 0.29975 | -0.008025
60s | 0.044403 | 0.12345 | 0.079421 | 0.035033 | 0.087402 | 0.1545 | 0.24892 | 0.77517 | 5.9407 | 32.9882 | 54.4518 | 55.7251 | 48.9131 | 39.1846 | 29.5547 | 22.5992 | 17.2991 | 13.1114 | 9.6796 | 7.199 | 5.2992 | 3.9298 | 2.9839 | 2.2973 | 1.788 | 1.3758 | 1.1474 | 0.93498 | 0.77748 | 0.61719 | 0.51881 | 0.5128 | 0.35897 | 0.29999 | 0.30266 | 0.28095 | 0.34461 | 0.23382 | 0.46932 | 0.33689 | 0.28061 | 0.24063 | 0.3043 | -0.17136 | -0.19571 | 0.31847 | 0.16185 | 0.051937
70s | 0.0089874 | 0.089652 | 0.025141 | 0.027954 | 0.010301 | 0.09296 | 0.19186 | 0.85821 | 10.9756 | 35.9836 | 33.5948 | 27.2097 | 22.901 | 18.792 | 14.7386 | 11.7331 | 9.4415 | 7.4825 | 5.8449 | 4.5238 | 3.5433 | 2.7356 | 2.1148 | 1.7052 | 1.3772 | 1.121 | 0.90558 | 0.77706 | 0.69788 | 0.51089 | 0.44315 | 0.47166 | 0.34866 | 0.3135 | 0.29408 | 0.34693 | 0.42148 | 0.26282 | 0.38085 | 0.19481 | 0.17262 | 0.37719 | 0.26017 | -0.12161 | -0.18258 | 0.094629 | 0.48758 | 0.54834
Chart: TE, 1mA
| 360 | 370 | 380 | 390 | 400 | 410 | 420 | 430 | 440 | 450 | 460 | 470 | 480 | 490 | 500 | 510 | 520 | 530 | 540 | 550 | 560 | 570 | 580 | 590 | 600 | 610 | 620 | 630 | 640 | 650 | 660 | 670 | 680 | 690 | 700 | 710 | 720 | 730 | 740 | 750 | 760 | 770 | 780 | 790 | 800 | 810 | 820 | 830
0s | 0.047455 | -0.045453 | 0.026824 | 0.0095938 | 0.025021 | 0.10076 | 0.57474 | 3.6503 | 7.4187 | 9.0026 | 6.7571 | 5.2907 | 4.7661 | 4.6251 | 4.4333 | 4.4604 | 4.4577 | 4.2483 | 3.8996 | 3.4607 | 2.9427 | 2.5193 | 2.0502 | 1.6962 | 1.386 | 1.1179 | 0.86725 | 0.73371 | 0.62858 | 0.49532 | 0.48167 | 0.37896 | 0.38912 | 0.31473 | 0.24108 | 0.047125 | 0.19468 | 0.27999 | 0.42293 | 0.24717 | 0.43478 | 0.38963 | 0.38077 | 0.0015317 | 0.034145 | 0.3731 | 0.19141 | 0.1426
10s | 0.025603 | 0.024419 | 0.021354 | 0.0058321 | 0.036823 | 0.092974 | 0.52628 | 3.3974 | 6.6808 | 8.1849 | 6.2552 | 5.1458 | 4.8795 | 4.8689 | 4.8357 | 4.862 | 4.9893 | 4.6987 | 4.2361 | 3.7626 | 3.2289 | 2.7085 | 2.1662 | 1.8112 | 1.4708 | 1.1534 | 0.96643 | 0.78033 | 0.6377 | 0.52424 | 0.54167 | 0.41918 | 0.37014 | 0.22851 | 0.26206 | 0.10728 | 0.1657 | 0.19659 | 0.20081 | 0.29844 | 0.36843 | 0.27118 | 0.46811 | -0.086074 | 0.63538 | 0.72817 | 0.056636 | 0.56853
20s | 0.025662 | -0.03813 | 0.040836 | 0.05013 | 0.067047 | 0.098152 | 0.46889 | 2.6552 | 4.9281 | 6.1883 | 5.274 | 5.038 | 5.5531 | 6.1234 | 6.451 | 6.7012 | 6.7564 | 6.4185 | 5.6985 | 4.9058 | 4.0665 | 3.3414 | 2.5976 | 2.0379 | 1.6233 | 1.3002 | 1.049 | 0.84777 | 0.66417 | 0.57221 | 0.58637 | 0.3779 | 0.42074 | 0.26097 | 0.29445 | 0.096939 | 0.15087 | 0.20938 | 0.25289 | 0.17572 | 0.24332 | 0.25014 | 0.25265 | 0.15609 | 0.82185 | 0.66839 | -0.49601 | 0.77929
30s | 0.050032 | -0.019464 | 0.030531 | 0.059656 | 0.046473 | 0.083114 | 0.37249 | 1.7458 | 3.0212 | 4.4549 | 5.1676 | 6.4771 | 8.6893 | 10.4319 | 11.1961 | 11.4862 | 11.2056 | 10.0432 | 8.4271 | 6.8749 | 5.3907 | 4.1982 | 3.1591 | 2.4034 | 1.8934 | 1.4366 | 1.1234 | 0.88435 | 0.70891 | 0.56082 | 0.54382 | 0.44636 | 0.38265 | 0.30735 | 0.3498 | 0.13225 | 0.20059 | 0.24192 | 0.33363 | 0.31312 | 0.33103 | -0.10806 | 0.18436 | 0.1629 | 0.411 | 0.7433 | -0.27147 | 0.20865
40s | 0.041088 | 0.048696 | 0.025465 | 0.060555 | 0.038748 | 0.046926 | 0.3046 | 0.98273 | 1.9083 | 4.8264 | 8.3329 | 12.9362 | 18.3338 | 21.348 | 21.5418 | 20.2122 | 17.8222 | 14.6193 | 11.1975 | 8.4385 | 6.2419 | 4.5939 | 3.4048 | 2.5369 | 1.9417 | 1.427 | 1.1434 | 0.89896 | 0.65584 | 0.58953 | 0.59977 | 0.41673 | 0.41278 | 0.28838 | 0.27907 | 0.12904 | 0.1628 | 0.22816 | 0.38454 | 0.29371 | 0.66018 | 0.3431 | 0.37668 | -0.19921 | 0.26977 | 1.062 | -0.053545 | -0.34194
50s | 0.055462 | 0.054465 | 0.12942 | 0.10376 | 0.086217 | 0.15335 | 0.22351 | 0.65283 | 2.1594 | 9.9933 | 21.0312 | 31.7394 | 38.7395 | 37.6187 | 31.6923 | 25.5567 | 19.9044 | 15.0009 | 10.8864 | 7.982 | 5.7134 | 4.2076 | 3.1088 | 2.2961 | 1.8012 | 1.4028 | 1.1249 | 0.85406 | 0.66237 | 0.57778 | 0.60974 | 0.42118 | 0.40301 | 0.31373 | 0.27528 | 0.1518 | 0.21472 | 0.4229 | 0.32723 | 0.44174 | 0.62236 | 0.38655 | 0.52461 | 0.062103 | 0.57667 | 0.20119 | -0.24145 | 0.18839
60s | 0.043771 | 0.041391 | 0.066628 | -0.0031814 | 0.063005 | 0.15813 | 0.22805 | 0.61089 | 4.5521 | 25.9156 | 43.9141 | 45.706 | 40.5382 | 32.5464 | 24.6614 | 18.8395 | 14.4645 | 10.9196 | 8.045 | 5.9763 | 4.4276 | 3.3092 | 2.5149 | 1.9768 | 1.539 | 1.2188 | 0.96872 | 0.76205 | 0.64203 | 0.5271 | 0.56669 | 0.44721 | 0.40861 | 0.25836 | 0.43685 | 0.10929 | 0.31514 | 0.19974 | 0.4404 | 0.61259 | 0.51787 | 0.31119 | 0.47478 | 0.1309 | 0.40369 | 0.46567 | -0.1171 | 0.39108
70s | 0.063555 | 0.037676 | 0.015829 | 0.09398 | 0.081713 | 0.093126 | 0.16162 | 0.71763 | 8.6772 | 29.279 | 27.5051 | 22.5495 | 19.0318 | 15.5935 | 12.2553 | 9.7659 | 7.8836 | 6.2101 | 4.7975 | 3.7418 | 2.9147 | 2.2965 | 1.7538 | 1.4368 | 1.1372 | 0.94843 | 0.8103 | 0.65015 | 0.5175 | 0.46413 | 0.47141 | 0.35908 | 0.42314 | 0.24967 | 0.28412 | 0.013704 | 0.30179 | 0.27411 | 0.30785 | 0.42892 | 0.5476 | 0.44854 | 0.36835 | 0.12966 | 0.27316 | 0.83629 | -0.14291 | -0.55902
Angle [°]
Angular spectra

## Slide 32
Emission zone location
Maxima angles

## Slide 33
Engineering Device Structures

## Slide 34
Device architecture
3D Illustration
Gate – Al
Dielectric – td
Patterned source – ts 100Å Au
Active layer
Drain – Al
Macro scale top view
500μm
100μm
100μm
L - Channel length - active layer thickness
D - Perforations’ diameter (~80nm)
FF - perforations area ratio
td & ts
Fundamental parameters
O. Globerman, "Lateral And Vertical Organic Field Effect Transistors," M.Sc., Electrical Engineering, Technion Israel Institute of Technology, Israel, 2006.

## Slide 35
How does it work?
Drain
Patterned source
Gate Insulator
Gate
VG > 0

## Slide 36
ON
Drain
Gate Insulator
Gate
hS
D=80nm
The effect of the perforations’ aspect ratio
VDS=1V
7
9
13
hS[nm]
(b)
Au
Al
C60
Φb0
h+
e-
S
SC
D
IG[A]
VDS=1V
(a)
Measurements
Simulations
φb0=0.68eV.
“Thick” source  Tunnel effect
A. J. Ben-Sasson, E. Avnon, E. Ploshnik, O. Globerman, R. Shenhar, G. L. Frey, and N. Tessler, "Patterned electrode vertical field effect transistor fabricated using block copolymer nanotemplates," Applied Physics Letters, vol. 95, p. 213301, 2009.
A. J. Ben-Sasson and N. Tessler, "Patterned electrode vertical field effect transistor: Theory and experiment," Journal of Applied Physics, vol. 110, p. 12, Aug 2011.
A. J. Ben-Sasson, Z. Chen, A. Facchetti, and N. Tessler, "Solution-processed ambipolar vertical organic field effect transistor," Applied Physics Letters, vol. 100, pp. 263306-4, 2012.

## Slide 37
“Fast” Switching
(L~170nm)
Stray Capacitance area 1X0.5mm.
VDS=10V
VGS=-10V  10V
Reducing stray serial resistance.
Better than 100kHz BW.

## Slide 38: Summary
In degenerate semiconductors part of the current is due to energy flow
(similar to the case of energy flow due to thermal gradient)
It is possible to have some level of “post-synthesis” manipulation of materials with the aim to provide “building blocks” for device engineering
Reducing the OLED’s micro-cavity emission to a simple expression allows for physical insight but more importantly – provides an engineering too.
Vertical Field Effect Transistors – low voltage , high current & fast

## Slide 39
Uri Banin, Asaf Aharoni
Hebrew Univ., Jerusalem
Yoav Eichen, Shai Tal
Technion
Jung Il Jin, Yang Jun Yu,
Korea Univ,
NCs
Peptides
Wide gap x-link
Antonio Facchetti, Zhihua Chen,
Polyera Corporation
Ntype (VOFET)
Israel Science Foundation
Israel Ministry of Science
Minerva Center
In Collaboration with:
Funding
Thank You

## Slide 40
Thomson effect, the evolution or absorption of heat when electric current passes through a circuit composed of a single material that has a temperature difference along its length. This transfer of heat is superimposed on the common production of heat associated with the electrical resistance to currents in conductors. If a copper wire carrying a steady electric current is subjected to external heating at a short section while the rest remains cooler, heat is absorbed from the copper as the conventional current approaches the hot point, and heat is transferred to the copper just beyond the hot point. This effect was discovered (1854) by the British physicist William Thomson (Lord Kelvin)
When carriers move from cold to hot they need to gain energy in order to be distributed in energy according to the new temperature. For that they absorb phonons (heat) and the conductor cools.