## Slide 1: Generation and Recombination in Organic Solar Cells
Lior Tzabari, Dan Mendels, Nir Tessler
Nanoelectronic center, EE Dept., Technion

## Slide 2: Outline
Macroscopic View of recombination P3HT:PCBM
- Exciton Annihilation as the bimolecular loss
Generalized Einstein Relation (one page)

## Slide 3
What about recombination in P3HT-PCBM Devices
Let’s take a macroscopic look and decide on the relevant processes.
What experimental technique would be best?
Picture taken from:
http://blog.disorderedmatter.eu/2008/06/05/picture-story-how-do-organic-solar-cells-function/ (Carsten Deibel)

## Slide 4: Mobility Distribution Function or Spatially Dispersive Transport
N. Rappaport et. al., APL, 88, 252117, 2006
N. Rappaport et. al., JAP, 99, 064507, 2006
N. Rappaport, et. al., Phys. Rev. B 76 (23), 235323 (2007).
L. S. C. Pingree, et.al., Nano Lett. 9 (8), 2946-2952 (2009).
Different time-scales
Different Populations
(PV is a CW device )

## Slide 5
Cell Efficiency
Generating Power (mWcm-2)
HOMO
Glass
ITO
PEDOT:PSS
Ca
Al
(If Undoped)
Only Loss Mechanism
Is
Exciton recombination
(Intra, Inter, “pairs”,…)
Free-Charge
Generation Efficiency
Other Losses Kick in
N. Tessler and N. Rappaport, JAP, vol. 96, pp. 1083-1087, 2004.
N. Rappaport, et. al., JAP, vol. 98, p. 033714, 2005.
QE as a function of excitation power

## Slide 6: QE as a function of excitation power Langevin /Bimolecular loss
N. Tessler and N. Rappaport, Journal of Applied Physics, vol. 96, pp. 1083-1087, 2004.
N. Rappaport, et. al., Journal of Applied Physics, vol. 98, p. 033714, 2005.
Charge generation rate
Photo-current
Bimolecular recombination-current
No re-injection
Signature of
bi-molecular Loss
Smaller Bimolecular Coefficient

## Slide 7
L. Tzabari, and N. Tessler, Journal of Applied Physics 109, 064501 (2011)
Nt – Density of traps.
dEt - Trap depth with respect to the mid-gap level.
Cn- Capture coefficient
LUMO
HOMO
Mid
gap
dEt
Bimolecular
Monomol
Doped  Traps already filled
Intrinsic (traps are empty)
QE as a function of excitation power SRH (trap assisted recombination) loss

## Slide 8
L. Tzabari, and N. Tessler, Journal of Applied Physics 109, 064501 (2011)
LUMO
HOMO
Mid
gap
Traps
Fewer Traps
Deeper Traps
QE as a function of excitation power SRH (trap assisted recombination) loss

## Slide 9
What can we learn using simple measurements
(intensity dependence of the cell efficiency)
Bi- Molecular
L. Tzabari, and N. Tessler, Journal of Applied Physics 109, 064501 (2011)
SRH (trap assisted)

## Slide 10: Recombination in P3HT-PCBM
4min | 
1.5e-12 | Kb[cm3/sec]
10
-2
10
0
10
2
0.55
0.6
0.65
0.7
0.75
0.8
0.85
0.9
0.95
1
4 min
Anneal
, - Experiment
, - Model
Intensity [mW/cm2]
Normalized QE
Kb – Langevin bimolecular
recombination coefficient
In practice detach it from its physical origin and use it as an independent fitting parameter
190nm of P3HT(Reike):PCBM (Nano-C)(1:1 ratio, 20mg/ml) in DCB
PCE ~ 2%
Notes: צריך קבוע יותר גדול – הגיוני כי הניידות גדלה.
אבל!!! מצד שני שינוי הניידות בלבד יביא לתוצאות הפוכות מאחר והגדלת הניידות מגדילה גם את יכולת האיסוף – וברגע שיכולת האיסוף גדלה כמות נושאי המטען האפקטיבית בהתקן קטנה ומנגנוני האיבוד נכנסים מאוחר יותר.
=> יכול להיות שינוי תלוי מורפולוגיה בלבד.

## Slide 11: Recombination in P3HT-PCBM
10min | 4min | 
8e-12 | 1.5e-12 | Kb[cm3/sec]
4 min
10 min
, - Experiment
, - Model
Notes: צריך קבוע יותר גדול – הגיוני כי הניידות גדלה.
אבל!!! מצד שני שינוי הניידות בלבד יביא לתוצאות הפוכות מאחר והגדלת הניידות מגדילה גם את יכולת האיסוף – וברגע שיכולת האיסוף גדלה כמות נושאי המטען האפקטיבית בהתקן קטנה ומנגנוני האיבוד נכנסים מאוחר יותר.
=> יכול להיות שינוי תלוי מורפולוגיה בלבד.

## Slide 12
Shockley-Read-Hall Recombination
LUMO
HOMO
Mid gap
, - Experiment
, - Model
4 min
10 min
L. Tzabari and N. Tessler, "JAP, vol. 109, p. 064501, 2011.
dEt
Intrinsic (traps are empty)
I. Ravia and N. Tessler, JAPh, vol. 111, pp. 104510-7, 2012. (P doping < 1012cm-3)

## Slide 13
Shockley-Read-Hall + Langevin
10min | 4min | 
1.2e17 | 1.9e17 | Nt [1/cm3]
0.371 | 0.435 | dEt [eV]
0.5e-12 | 0.5e-12 | Kb[cm3/sec]
4 min
10 min
, - Experiment
, - Model
LUMO
HOMO
Mid
gap
dEt
The dynamics of recombination at the interface is both
SRH and Langevin

## Slide 14
Exciton Polaron Recombination
Neutrally excited molecule (exciton) may transfer its energy to a charged molecule (electron, hole, ion).
As in any energy transfer it requires overlap between the exciton emission spectrum and the “ion” absorption spectrum.
M. Pope and C. E. Swenberg, Electronic Processes in Organic Crystals., 1982.

## Slide 15
A. J. Ferguson, N. Kopidakis, S. E. Shaheen and G. Rumbles, J Phys Chem C 112 (26), 9865, 2008
Quenching of Excitons by Holes in P3HT Films
In neat P3HT ramping the excitation power results in exciton-exciton annihilation
Add 1% PCBM and losses become dominated by Exciton-Polaron recombination.
Excitation Density
Generated Charge Density (at t=0)
Kep=3x10-8 cm3/s

## Slide 16
Exciton Polaron Recombination
Nt – Density of traps.
dEt - trap depth with respect to the mid-gap level.
Kep – Exciton polaron recombination rate.
Kd– dissociation rate 1e9-1e10 [1/sec]
Sensitivity | 10min | 4min | 
0 | 1.05e17 | 1.9e17 | Nt [1/cm^3]
0.015 | 0.365 | 0.435 | dEt [eV]
1.08e-8 | 1.6e-8 | 1.6e-8 | Kep[cm^3/sec]
4 minutes
10 minutes
, - Experiment
, - Model
A. J. Ferguson, et. al., J Phys Chem C, vol. 112, pp. 9865-9871, 2008 (Kep=3e-8)
J. M. Hodgkiss, et. al., Advanced Functional Materials, vol. 22, p. 1567, 2012. (Kep=1e-8)

## Slide 17
T. A. Clarke, M. Ballantyne, J. Nelson, D. D. C. Bradley, and J. R. Durrant, "Free Energy Control of Charge Photogeneration in Polythiophene/Fullerene Solar Cells: The Influence of Thermal Annealing on P3HT/PCBM Blends," Advanced Functional Materials, vol. 18, pp. 4029-4035, 2008. (~50meV stabilization)
4 minutes
10 minutes
Sensitivity | 10min | 4min | 
0 | 1.05e17 | 1.9e17 | Nt [1/cm^3]
0.015 | 0.365 | 0.435 | dEt [eV]
1.08e-8 | 1.6e-8 | 1.6e-8 | Kep[cm^3/sec]
Traps or CT states are stabilized during annealing

## Slide 18
Bias Dependence
10 minutes anneal
Charge
Generation
- Generation
- Recombination
- Mobility

## Slide 19: What does it all mean (summary, conclusions,…)
Charge generation requires some field and this is observed at very low light intensities
The “geminate” recombination occurs through “defect sites” and their availability limits the recombination.
“Defect sites” or “Traps” act like stabilized charge transfer states.
At high enough density (depending on morphology) a new channel opens up and Losses become Bi-molecular.
Bi-molecular = electron-hole or exciton-polaron?

## Slide 20
Disordered hopping systems
degenerate semiconductors
Y. Roichman and N. Tessler, APL, vol. 80, pp. 1948-1950, Mar 18 2002.
White Dwarf
Astronomy: Degenerate gas pressure.
Fluidics: Osmosis
To describe the charge density/population one should use Fermi-Dirac statistics and not Boltzmann
Degenerate
It’s effect is in basic thermodynamics texts.
Drift
Diffusion
Seebeck
Streaming
In Semiconductors:
Diffusion
Streaming
Enhanced
Diffusion
D. Mendels and N. Tessler, J. Phys. Chem. C 117 (7), 3287-3293 (2013).
Degenerate (gas)
Degenerate (gas) Pressure
 Pressure = Enhanced Diff.

## Slide 21: Thank You
Israeli Nanothecnology Focal Technology Area on "Nanophotonics for Detection"
Ministry of Science, Tashtiyot program
Helmsley project on Alternative Energy of the Technion, Israel Institute of Technology, and the Weizmann Institute of Science

## Slide 22
Charge recombination is activated

## Slide 23: Why Generalized Einstein Relation does not affect the Ideality Factor of PN Diode
In Amorphous semiconductors:
Long Diode [N. Tessler and Y. Roichman, Org. Electron. 6 (5-6), 200-210 (2005)]
Short Diode
[Y. Vaynzof, Y. Preezant and N. Tessler, Journal of Applied Physics 106 (8), 6 (2009)]
Exponential DOS