## Slide 1: VFET – A Transistor Structure for Amorphous semiconductors
Michael Greenman, Ariel Ben-Sasson, Nir Tessler
Sara and Moshe Zisapel Nano-Electronic Center, EE Dept., Technion Israel Institute of Technology, Haifa, Israel

## Slide 2
L. P. Ma and Y. Yang, Appl. Phys. Lett. 85 (21), 5084 (2004).
Vertical Transistors
Vertical-junction field-effect transistor
D. C. Mayer, N. A. Masnari, and R. J. Lomax, Ieee Transactions on Electron Devices 27, 956-961 (1980).
Yang, Y.; Heeger, A. J. Nature 1994, 372, (6504), 344-346.
Patent US841387 from 10/25/1906
Vacuum tube triode
Solid state triode
(AKA SCLT)
Vertical Organic FET
III

## Slide 3
Source
Si++
SiO2
Source
Semiconductor
Drain
L
Gate
Si++
SiO2
Gate
Drain
Source
Lateral
FET:
Vertical
FET:
Lateral Goes Vertical
Channel Length
Direction
Location
Drain
L
Ma, L. & Yang, Y. Applied Physics APL 85, 5084 (2004).

## Slide 4
Conductive; Transparent
Source electrode characteristics
L
Perforated conductive layer
A. J. Ben-Sasson et al., Applied Physics Letters 95, 213301 (2009).
VOFET Architecture
Patterned source electrode
III
Virtual electrode

## Slide 5
Processes:
Block-copolymers
fPMMA
fPS
Di-block copolymer self-assembly

## Slide 6
Processes - Block-copolymers
Annealing
Disordered to molecularly organized
Thermal annealing
Solvent annealing
[T↑, TG const.]
[T const., TG↓]
3µm

## Slide 7
Block-copolymers as photolithography masks
Design tools:
Chemistry
Dimensions
Process
Processes:
Block-copolymers
IV

## Slide 8
Creating patterned source electrode using block co-polymers (BCP) lithography.
PS
PMMA
PMMA
PS
PS
Au
Au
Ben-Sasson, A. J. et al. Patterned electrode vertical field effect transistor fabricated using block copolymer nanotemplates. Applied Physics Letters 95, 213301 (2009).
Works on cm scale samples
Notes: Ariel ben sasson devloped a self assmblend block copolymer process to fabricate a pattrernd source electrode. This method is based on a phase-sepration between the 2 differ block in the polymer which aquirs under certain annealing process. A differ sencebility to UV light is used to remove the PMMA matrix leaving a standing cyclnders of PS. Then a thin ti/au is evperate on the PS cylders. Using lift-off process the PS cylnders is removed leaving the desire pattern electrode. The patterned electorde is not only transperte to DC electric field but also for a visible light there for is hard to seen on the samples. Keep in mind the resistance of this electrode is not neglebal becouse the relativly high sheet resistance.

## Slide 9
Device architecture
3D Illustration
Gate – Al
Dielectric – td
Patterned source – ts 100Å Au
Active layer
Drain – Al
Macro scale top view
500μm
100μm
100μm
L - Channel length - active layer thickness
D - Perforations’ diameter (~80nm)
FF - perforations area ratio
td & ts
Fundamental parameters
O. Globerman, M.Sc. Thesis, Electrical Engineering, Technion, Israel, 2006
A. J. Ben-Sasson and N. Tessler, Nano Letters, vol. 12, pp. 4729-4733, 2012/09/12 2012.

## Slide 10
How VOFET works?
Our approach – patterned source electrode:
Sze, S. & Ng, K. Physics of semiconductor devices. (2006).

## Slide 11
Drain
Patterned source
Gate dielectric
Gate
Charge density in the Semiconductor layer for
Unbiased gate
Virtual contact
Formation
Saturated virtual contact
OFF
OFF
ON
How VOFET works?
Off state – Contact Limited due to Schottky barrier
On state – Virtual contact, Space Charged Limited Current

## Slide 12
Potential surface
Electric field
Charge distribution
Virtual contact
Vertical Channel
Design: Schottky (On current)

## Slide 13
The effect of the perforations’ aspect ratio
VDS=1V
7
9
13
hS[nm]
(b)
Au
Al
C60
Φb0
h+
e-
S
SC
D
IG[A]
VDS=1V
(a)
Measurements
Simulations
“Thick” source  Tunnel effect
Drain
Patterned source
Gate dielectric
Gate
ON

## Slide 14
The Electrode Barrier
High barrier  High On/Off
High barrier  High VTO
On and Off channel spatial origin is different
A. J. Ben-Sasson, N. Tessler, Journal of Applied Physics 110, 044501 (2011).
Φb
VOn

## Slide 15
Non-uniform structure
JOff
JOn
V.B
VOn
VOn
JOff
Stractured electrode

## Slide 16
DC characteristics
Solution processed active layer:
Ben-Sasson, A. J., Chen, Z., Facchetti, A. & Tessler, N. Solution-processed ambipolar vertical organic field effect transistor. Applied Physics Letters 100, 263306 (2012).
Reducing Vg:
A. Ben-Sasson, G. Ankonina, M. Greenman , M. T. Grimes and N. Tessler , Low-temperature molecular vapor deposition of ultra-thin metal oxide dielectric for low-voltage vertical organic field effect transistors, ACS Appl Mater Interfaces (2013)
4.08 eV
4.0 eV
5.6 eV
5.1 eV
Drain (Al)
N2200
Source(Au)
Active
Source
Gate
Drain

## Slide 17
Silver Nanowire Based Electrode

## Slide 18
Silver Nanowire Based Electrode

## Slide 19
Scope
ch1
Voltage Amplifier
Scope
ch2
VFET
Assembling time-resolved setup
reducing source resistance
Time resolved measurement
Greenman, M., Ben-Sasson, A. J., Chen, Z., Facchetti, A. & Tessler, N. Fast switching characteristics in vertical organic field effect transistors. Appl. Phys. Lett. 103, 073502 (2013).
Notes: So whwn we minimize the area of the patterned source only to the device area we could reveal a much fater response of 2 micro-sec. This time the limiting pramter was the ringing effect in the setup. We had use some low pass filter to analize the result which increase the result of the turn on time. But still almost 2 orders of magnetude faster the the privace measurment.

## Slide 20
Time-resolved simulation
Time resolved measurement
Greenman, M., Ben-Sasson, A. J., Chen, Z., Facchetti, A. & Tessler, N. Fast switching characteristics in vertical organic field effect transistors. Appl. Phys. Lett. 103, 073502 (2013).
m=10-3cm2V-1s-1
m=10+1cm2V-1s-1
ns turns into ps
Notes: Usng time resolved numrical simulation we thinks the intrinsic turn on time of the device is faster. Somewhere between 2-5 TOF depending on the ds voltage. Placing the device pramters in the TOF formola leads to 16-32 ns meaning a much better turn on time should be revlead but is hiden due to setup and overlap technicals problems

## Slide 21
Silver Nanowire Based Electrode

## Slide 22
Silver Nanowire Based Electrode
A. J. Ben-Sasson et al., Self-Assembled Metallic Nanowire-Based Vertical Organic Field-Effect Transistor. ACS Appl. Mater. Interfaces 7, 2149-2152 (2015)

## Slide 23
Standard photo-lithography
Replacing BCP technic with basic lithography:
Fits for metric scale substrates. (matches for standard FAB lines)
Enables more complex lift-off or etching process.
Holes diameter:

## Slide 24
Holes diameter effect
Standard photo-lithography
Unit cell
Fill Factor
Perimeter per unit cell
Perimeter per device area
Perimeter Area = Injection Area
Diameter

## Slide 25
Connecting VOFET’s to invertor:
Conventional photo-lithography
The first VOFET invertor!
Not good but still invert the signal.
Low performance due to P-VOFET strong off current.

## Slide 26: Thank You
The fabrication was performed at the Micro-Nano Fabrication Unit (MNFU), Technion.